## Slide 1: Study of two-particle response and phase changes in strongly correlated systems using Dynamical Mean Field Theory
Bismayan Chakrabarti
Dissertation defense
Supervisor: Prof. Kristjan Haule

## Slide 2: Contents
Why are strongly correlated systems interesting?
Why DFT+DMFT?
Individual Research projects using DFT+DMFT-
  Calculation of Magnetic Spectral Function
    Volume collapse transition in Cerium
    The valence fluctuating ground state of - Pu
  Spin state transition in LaCoO3
  Inadequacy of cRPA in estimating screening of interactions

## Slide 3: Condensed Matter- The study of Emergence
Traditional guiding light of Western Science: Reductionism
“Human science fragments everything in order to understand it, kills everything in order to examine it. ” ― Leo Tolstoy, War and Peace

## Slide 4: Condensed Matter- The study of Emergence
Condensed Matter: More is different – P.W. Anderson (1972)
Emergence: Collections of entities exhibit properties not trivially understood from properties of individual constituents.
Condensed Matter: The study of emergent phenomenon in material systems

## Slide 5: Can we understand macroscopic systems?
Fundamental equation governing the physics of all materials known in principle - Schrodinger Equation:
Can’t solve for macroscopic systems even with most powerful computers. Too many degrees of freedom (~10^23)
We must find efficient approximation schemes to make calculations computationally tractable

## Slide 6
The underlying physical laws necessary for the mathematical theory of a large part of physics and the whole of chemistry are thus completely known, and the difficulty is only that the exact application of these laws leads to equations much too complicated to be soluble. It therefore becomes desirable that approximate practical methods of applying quantum mechanics should be developed, which can lead to an explanation of the main features of complex atomic systems without too much computation-Paul Dirac (1929)

## Slide 7: Electronic correlations
Materials with open s or p shells – Weak electronic Correlations.
  Landau Fermi Liquid Theory works well.
  Density Functional Theory (DFT) extremely successful even with simplistic treatment of electronic correlations.
  Put in Kohn Sham Pics
Materials with open d or f shells:
  More localized electrons! Stronger Electronic Correlations
  DFT Fails !
  Must formulate alternate methods

## Slide 8: Strongly correlated systems
Most Famous model to study strong correlations: Hubbard Model
Interesting Physics in intermediate regime- Interplay of localization/itineracy
U / t ~ 0
U / t >>1
Itinerant
Localized
Strongly Correlated Materials
U / t ~ O(1)
Metal-insulator transition
High Tc superconductivity
Heavy fermions.
Highly complex phase diagrams!!

## Slide 9: The DMFT approximation
Simulating strongly correlated systems hard: Solve true many body equation?
No! Use Dynamical Mean Field Theory (DMFT)
Lattice Problem with interactions
Impurity coupled to self-consistently determined bath
Computational impurity solvers exist!
Exact in infinite dimensional limit

## Slide 10: The DMFT approximation: An alternative approach
Baym Kadanoff Functional
Stationary value at Physical Greens function Free Energy of System

## Slide 11
Full Luttinger Ward Functional:
DMFT Approximation- Replace all Greens functions by Local Greens functions
Self Energy Becomes Local

## Slide 12: Merging DFT with DMFT
DMFT good at dealing with local correlations: treat d and f shells
  Too computationally expensive to treat all orbitals
DFT excellent for weakly correlated orbitals
  Computationally cheap but can’t simulate correlated orbitals
Combine them DFT+DMFT : State of the art method to perform ab initio simulations of correlated materials
DFT
DMFT
DFT+DMFT

## Slide 13: DFT+DMFT
Allows us to perform ab-initio simulations of actual material systems with open d or f shell elements
Allows for finite temperature simulations unlike DFT
State of the art impurity solvers allow a wide variety of experimental observables to be calculated
Caveats-
  Can be computationally expensive (f-shell elements like Pu require hundreds of thousands of computer hours)
  For some impurity solvers, require analytic continuation
  Double Counting: Eliminate the part of electronic correlations that are captured by both DMFT and DFT to avoid over-estimation of Coulomb term

## Slide 14: Selected Research Projects using DMFT

## Slide 15: Calculation of Magnetic Spectral function
The Magnetic Spectral function gives us information about all the magnetic excitations of the system. Can be measure by Neutron scattering experiments.
For materials with strong localization:
: Magnetic form factor
Imaginary part of Dynamic Magnetic Susceptibility
DFT+DMFT allows us to calculate , which we shall use to study two long standing problems in condensed matter
  The volume collapse transition in Cerium
  The valence fluctuating ground state in -Pu

## Slide 16: Volume Collapse transition in Cerium
Increase Pressure
-Ce -Ce transition in Cerium. Intensely studied for decades!
-Ce shows Pauli like susceptibility while -Ce shows Curie like susceptibility.
Possible explanations:
  Promotional Model (Coqblin et.al, 1968)
  Mott Transition (Johansson,1974)
  Kondo volume collapse (Lavagna et. al 1982. Allen et.al 1982)

## Slide 17: The form factor puzzle
Murani et.al (PRL 95, 256403):
Form factor remains unchanged across transition
LDA calculation assuming 4f electron forms itinerant band
4f electrons remain correlated across the transition!
Disagrees with DFT

## Slide 18: DMFT results for FM(q)
DMFT results in perfect agreement with experiment!

## Slide 19: DMFT results for
Moves to higher for -Ce
Increased TK
Local moment peak at
Increased Hybridization

## Slide 20: DMFT results for
Almost perfect Agreement!

## Slide 21: The valence fluctuating ground state of -Pu
Plutonium has a highly complex phase diagram.
Pauli Susceptibility
Anomalously high Cv
Theories which reproduce unit cell volume predict static moment
Experiments disagree!
“Missing magnetism of -Pu”

## Slide 22: Magnetic Form Factor & Valence fluctuations
Large fluctuations in occupation of 5f orbital- captured by DMFT
Put in my citation

## Slide 23: The Missing magnetism
Peak at
T>TK
T<TK
At room Temperature Magnetic moment is screened by Kondo cloud

## Slide 24
Almost perfect Agreement!

## Slide 25: Spin state Transition in LaCoO3

## Slide 26: Why LaCoO3?
LaCoO3 is a perovskite (ABO3) with La on the A site and Co on the B site surrounded by Oxygen Octahedra.
The Octahedra undergo out of phase rotations along the [111] axis (a-a-a- tilt pattern)
Narrow band-gap insulator at low temp (<60K) with Pauli-like susceptibility.
Between 90-150 K, transitions to a local moment phase with Curie-Weiss like susceptibility. Gradual closing of the insulating gap, known to be metallic above 600K.
La
Co
O

## Slide 27: Why LaCoO3?(contd..)
The main puzzle is to determine the spin state of the nominally 3d6 Co ion which characterizes the local moment phase at high temperature.
Much disagreement between theoretical approaches. Experiments have also not been able to unambiguously settle the issue
Must also explain the non-concurrent metal-insulator transition taking place at higher temperature than spin state transition.
(“ Low to Intermediate Spin”)
(“ Low to High Spin”)
eg
eg
t2g
t2g

## Slide 28: Aim of our Project
Fully charge self-consistent DFT+DMFT on LaCoO3 in order to investigate the true nature of the Spin State (SS) transition and Metal-Insulator transition (MIT) in LaCoO3.
Wien-DMFT package developed at Rutgers. DMFT on top of Wien2k DFT package. Numerically exact state-of-the-art CTQMC impurity solver
Importance of structural factors such as octahedral rotations and thermal expansion in bringing about the transitions.
Importance of electronic entropy in stabilizing the local moment phase of LaCoO3.

## Slide 29: Structures studied
To study the effects of octahedral rotations and thermal expansion on the transitions, we study 4 different structures
  Structures from neutron scattering experiments (Thornton et. al).
    Low Temperature Structure at 4 K (LTa- structure).
    High Temperature Structure at 1143 K (HTa- structure)
  Fictitious Structures with no octahedral rotations (a0a0a0 pattern)
    With same lattice vectors as 4K structure (LTa0 structure)
    With same lattice vectors as 1143 K structure (HTa0 structure)
For all 4 structures we perform simulations at temperatures between 116K and 1160 K.

## Slide 30: Density of States
We see a clear metal insulator transition as a function of temperature in all but the LTa0. Considerable overlap between t2g and eg orbitals at high temperature.
HTa-
T=116K
T=1160K

## Slide 31: Density of States
We see a clear metal insulator transition as a function of temperature in all but the LTa0. Considerable overlap between t2g and eg orbitals at high temperature.
LTa-
T=116K
T=1160K

## Slide 32: Density of States
We see a clear metal insulator transition as a function of temperature in all but the LTa0. Considerable overlap between t2g and eg orbitals at high temperature.
HTa0
T=116K
T=1160K

## Slide 33: Density of States
We see a clear metal insulator transition as a function of temperature in all but the LTa0. Considerable overlap between t2g and eg orbitals at high temperature.
LTa0
T=116K
T=1160K

## Slide 34: Measuring the Spin state
The CTQMC impurity solver gives probabilities of the 1024 different states of the Co 3d orbital. allows us to calculate the expectation value of |SZ|.
We find that the actual occupancy of the Co d orbital is ~6.6 due to hybridization with O atoms which results in large valence fluctuations.
Not accurate to think of the spin state in terms of only the d6 state!
We measure the evolution of the Probability of all values of |SZ|as a function of temperature for all 4 structures.

## Slide 35: The Spin State Transition!!
Earliest & Strongest Transition in HTa-
Almost NO Transition in LTa0
Transition Temp higher than Expt!

## Slide 36: Non-concurrent Transitions!!
Tss HTa-
TMIT HTa-

## Slide 37: Which Multiplet is to blame?
Tss
Tss
Tss
Tss
HS excitation
HS excitation
HS excitation
HS excitation
HTa-
HTa0
LTa0
LTa-

## Slide 38: Importance of Electronic Entropy
According to entropy driven scenario, LaCoO3 prefers higher spin multiplets due to Entropy gain.
To test effect of structural factors on electronic entropy we compute the Entropy difference between LTa- and HTa- structures at 1160K using state of the art Entropy calculation technique(Birol et.al)
Gain in TS of 110 meV per formula unit in HTa- compared to LTa- structure. Stabilizes HTa- structure
Shows that electronic entropy is vital in stabilizing the thermal expansion and driving the spin state transition in the material.
HTa-
LTa-
LTa-
HTa-
Energy
(E)
Free Energy
(F)
F=E-TS
1160K

## Slide 39: Conclusions
We performed fully charge self-consistent DFT+DMFT calculations on LaCoO3 to study the spin state and metal-insulator transitions.
Obtained non-concurrent spin state and metal-Insulator transitions. However spin state transition occurs at slightly too high temperature.
Determined that HS state is the first to get excited at the onset of the spin state transition for all occupancy sectors.
Larger octahedral rotations and lattice expansion favor the spin state transition.
Studied the importance of electronic entropy and found it to be essential in driving the structural transitions in the material.

## Slide 40: Thank You